## Slide 1
*Previous collaborators
Autonomous laboratory for sustainable research and discovery of new materials
Sašo Šturm
Belisa Alcantara Marinho, Kristina Žagar Soderžnik, Barbara Ljubec Božiček, Lara Einfalt, Benjamin Podmiljšak, Matej Komelj, Nejc Skoporc, Miran Čeh
Luka Suhadolnik*, Živa Marinko*
Development of new high-entropy-oxide catalysts by the anodic oxidation of high-entropy alloys

## Slide 2
Department for nanostructured materials:
at the forefront of basic research and innovation in materials
55: staff members 12: academic habilitation
39: reaserchers&postdocs 13: PhD students
Revenue: ̴3M € (40% / 27% / 30% / 3%)
National research programs: 3
ARIS projects/Weave: 26
Industry: 11
Cost/EIT/HE: 21
EU patent granted: 6
EU patent pending: 3
Equipment purchase (2018-2022): ̴1M+ €
2022-2023
Magnetic materials
and Intermetallics
Electron microscopy and materials modeling
Organic toxin sensors
Catalysis
Fusion
Advanced engineering and bio materials
Microplastics
Nanomedicine
Functional ceramics
Societal Challenges

## Slide 3
Challenges & prospects
Park, M., Leahey, E., & Funk, R. J. (2023). Nature, 613(7942), 138-144.
CD index: If an article is disruptive, subsequent papers will no longer cite the predecessors (the references of that article), where [1]: disruptive and [-1] consolidation work.
Are we in the decline of disruptive science?
Decline of CD index over time
Societal Challenges

## Slide 4
Merchant, Amil, et al. "Scaling deep learning for materials discovery." Nature 624.7990 (2023): 80-85.
Scientists know of about 48.000 different crystals. DeepMind has created a machine-learning tool called gnome (Graph Networks for Materials Exploration) that can use existing libraries of chemical structures to predict new ones. It came up with 2.200.000 crystal structures, each new to science.
Are we in the decline of disruptive science?
Challenges & prospects
Societal Challenges

## Slide 5
Park, M., Leahey, E., & Funk, R. J. (2023). Nature, 613(7942), 138-144.
Are we in the decline of disruptive science?
The decline in disruptive science ≠ decline in the quality of science
Possible causes of the decline:
The theory of “low-hanging fruit” assumes that most discoveries have already been made.
The increasing burden of knowledge & the tendency toward ultra-specialization.
Growing difficulty in securing research funds (discouraging riskier projects).
Correlation to materials science trends & straightforward solutions
Not true: 41 of the 58 ML predicted compounds were synthesised in a little over two weeks.
A pressing need for ”truly” interdisciplinary research
Improving the “research yield per research cost unit”
Challenges & prospects
Societal Challenges

## Slide 6
Autonomous laboratory for sustainable research and discovery of new materials
To reshape materials discovery by establishing an autonomous lab dedicated to sustainable research and the development of new materials.
Motivation

## Slide 7
Autonomous laboratory for sustainable research and discovery of new materials
General concept
The research concept will be dominated on an inverse materials design approach, where the desired end material property drives the entire discovery process.
Electrochemical-based synthesis
  Anodic oxidation
    Synthesis of thin films
      Applications in energy and environmental fields
  Electrochemical characterisation
    Cyclic voltammetry (CV), Linear sweep voltammetry (LSV), Electrochemical impedance spectroscopy (EIS), Chronoamperometry, Photoelectric conversion efficiency ()…
Autonomous LAB

## Slide 8
2011
Anodic oxidation
process
Metal foil
anodized area of 0.79 ± 0.03 cm2
anodized area of 50 cm2
Starting material: Metal foil/substrate/rod, etc.
Desired material: Immobilized nanostructured oxide material
Synthesis approach: Versatile anodic oxidation process
Desired property: Excellent photo/photo-electro/electro -catalytic response
Acknowledgement: Kristina Žagar Soderžnik
Roadmap: The research platform for catalytically active nanostructured oxide materials
Anodic oxidation process

## Slide 9
Roadmap: The research platform for catalytically active nanostructured oxide materials
2011
Anodic oxidation
process
Anodization of
single elements
Acknowledgement: Kristina Žagar Soderžnik
Anodic oxidation process
Starting material: Metal foil/substrate/rod, etc.
Desired material: Immobilized nanostructured oxide material
Synthesis approach: Versatile anodic oxidation process
Desired property: Excellent photo/photo-electro/electro -catalytic response

## Slide 10
Roadmap: The research platform for catalytically active nanostructured oxide materials
2011
Anodic oxidation
process
Anodization of
single elements
Nanostructured thin films
Anodic oxidation process
Starting material: Metal foil/substrate/rod, etc.
Desired material: Immobilized nanostructured oxide material
Synthesis approach: Versatile anodic oxidation process
Desired property: Excellent photo/photo-electro/electro -catalytic response

## Slide 11
Roadmap: The research platform for catalytically active nanostructured oxide materials
2011
Anodic oxidation
process
Anodization of
single elements
Environmental
applications
Nanostructured thin films
Activity of TiO2 nanotubes:
degradation of organic polutant
A non-exhaustive list of processing parameters:
Anodic oxidation process
Starting material: Metal foil/substrate/rod, etc.
Desired material: Immobilized nanostructured oxide material
Synthesis approach: Versatile anodic oxidation process
Desired property: Excellent photo/photo-electro/electro -catalytic response

## Slide 12
2011
Anodic oxidation
process
Anodization of
single elements
Environmental
applications
Nanostructured thin films
2022
New class of
materials
Exploring new
applications (energy)
Great opportunity, great challenges: High-Entropy Materials
Promising catalyst material
HEA ⟶ HEO
Atomic-scale disorder ⟶ enhanced kinetic properties
Abundant active sites ⟶ different types of catalytic reactions
Thermally stable, mechanically strong and corrosion - resistant
High entropy alloys (HEA)
Simultaneously proposed by Cantor1 and Yeh2 in 2004.
Possible HEA BCC: 30.2013
High entropy oxides (HEO)
First described in 2015 by Rost4.
Abundant active sites
For theoretical Ru0.2Ti0.2Ir0.2Os0.2Rh0.2O2 rutile HEO:
- estimated 1.95106 different adsorption sites5.
Applications in catalysis
The existence of abundant and customizable catalytic active sites makes HEAs and HEOs excellent catalysts for different reactions6.
1Cantor, B. et al. , Mater. Sci. Eng. A., 2004, 375–377, 213; 2Yeh, J.W. et al. , Adv. Eng. Mater., 2004, 6, 299; 3Chen, Wei, et al. "A map of single-phase high-entropy alloys." Nature Communications 14.1 (2023): 2856.
4Rost, C.M. et al. , Nat. Commun., 2015, 6; 5Svane, K.L. and J. Rossmeisl , Angew. Chemie Int. Ed., 2022, 61, e202201146; 6M. Anandkumar, J. Alloys Compd., 2021, 850, 156716.
[ Possible active sites: ～ 1M ]
x
[ Possible HEA/HEO: ～ 30k ]
⇒ (possible pathways)

## Slide 13: High Entropy Materials
B.L. Božiček et al., Journal of Materials Science 2024, doi.org/10.1007/s10853-024-09710-5
 | (Co,Fe,Ni,Mn,Cr)3O4 (this work) | (Co,Fe,Ni,Mn,Cr)3O4 (Einert et al., 2022) | (Co,Cu,Fe,Mn,Ni)3O4 (Wang et al., 2019) | RuO2 (Ma et al., 2022) | Reference values (SOTA materials)
Onset potential | 1.57 V | 1.58 V | 1.58 V | 1.47 |  1.61 V
Overpotential (at 10 mA/cm2) | 341 mV | 350 mV | 350 mV | 235 mV |  380 mV1
Tafel slope | 50 mV/dec | 35 mV/dec | 59.5 mV/dec | 77.2 mV/dec | 30 - 120 mV/dec2
2011
Anodic oxidation
process
Anodization of
single elements
Environmental
applications
Nanostructured thin films
2022
New class of
materials
Exploring new
applications (energy)
2024
Recent study: (Co,Fe,Ni,Mn,Cr)3O4 High-Entropy Oxides
1Scott, et al. "Energy & Environmental Science 15.5 (2022): 1977-1987.
2Kapałka, et al., Electrochemistry Communications, 10(4), 607-610.

## Slide 14
Conceptualization of an autonomous laboratory for sustainable research and discovery of HEO catalysts
The unique advantageous position at the JSI: strong tradition in material processing, DFT modelling, robotics, automation and knowledge technologies, all in one confined place.
Automatization
Testing
Synthesis
Caractherization

## Slide 15
The heart of the system: The state-of-the-art fume hood
Conceptualization of an autonomous laboratory
Two main functionalities:
automated synthesis
automated characterisation
Custom-built facility for the autonomous synthesis and electrochemical characterization of materials (12 m2)

## Slide 16
1 - multiplexer
2 - power supply
3 - electropolishing device
4 - fume cupboard (anodisation and photo-electro-catalysis)
5 - gas regulators
6 - storage cabinet
7 - chemical/electrolyte cabinet/chamber
State before renovation
Window
Entrance

## Slide 17
Current state

## Slide 18
Robot on a linear track

## Slide 19
Custom-built electrochemical cell

## Slide 20
The state-of-the-art fume hood: 15 functionalised sub-units

## Slide 21
Initial testing – workflow for autonomous laboratory
Raw material (R)
Metallic Ti foil
AO + Annealed material (AO+AN)
TiO2 crystalline nanotubes
Characterised material (C)
Electrochemical characterisation of AO+AN material
Anodised material (AO)
TiO2 amorphous nanotubes
Synthesis
Characterisation
Preparation
Anodisation
Annealing
Characterisation

## Slide 22
Future plans

## Slide 23
Autonomous laboratory for sustainable research and discovery of new materials at IJS
Leading Institutions and projects on Autonomous Research of Materials around the world
1988: Matsuda
Robot: Desktop robotic arm.
Finding: Optimized analytical colorimetric tests; first automated research report.
2009: King
Robot: Laboratory system with robots.
Finding: Identified genes for 13 orphan enzymes; hypotheses generated and tested autonomously.
2013: Desai
Robot: Flow reactor with automation.
Finding: Accelerated drug discovery; novel template identified for kinase inhibitors.
2016: Nikolaev
Robot: Laser-based system.
Finding: Optimized synthesis parameters for carbon nanotubes.
2020: Burger
Robot: Mobile robot.
Finding: Enhanced photocatalysts for hydrogen production; 6x more effective.
2020: Shimizu
Robot: Robot arm and sputtering system.
Finding: Optimized TiO2 films; reduced resistance using machine learning.
2023: Szymanski
Robot: Full robotic arms sequence.
Finding: Produced over 51 types of inorganic powders; integrated machine learning improved synthesis success.
First autonomous laboratory for materials research in Slovenia.
Thank you for your attention!
For more info, please contact me at: saso.sturm@ijs.si

## Slide 25
2011
Anodic oxidation
process
Anodization of
single elements
Environmental
applications
Nanostructured thin films
2022
New class of
materials
Exploring new
applications (energy)
2024
Integration with DFT
AI and automatization
Autonomous laboratory for rapid material discovery
Great opportunity, great challenges: High-Entropy Oxides (HEO)
Anode
(RuO2/IrO2/NiO)
Cathode
(Pt)
Electrocatalytic water splitting
H+
H2O
O2
OER
HER
+
-
Renewable
energy source
H2

## Slide 26
Material discovery: HEO catalyst for water-splitting reactions to generate green hydrogen
 | (1)
 | (2)
 | (3)
 | (4)
 | (1)
 | (2)
 | (3)
 | (4)
First simple questions:
What are the most efficient reaction pathways?
Not-so-straightforward answer:
1.95x106 – 6x109 different possible active sites
*
M
M
B
B
B
B
S
S
A rough estimate of possible local environments for an active adsorption site (*), considering only the nearest neighbour metal sites:
5 metal atoms forming HEO,
2 neighbour metal atoms (M),
4 bridge atoms (B),
2 sub-surface atoms (S)
59 ∼ 1.95x106 … and this is only for one compound!
The conventional pathways for the OER:
* active adsorption site

## Slide 27
Material discovery: HEO catalyst for water-splitting reactions to generate green hydrogen
Second simple questions:
How many high-entropy alloys could theoretically exist in a stable form for AO to HEO?
Not-so-straightforward answers:
Possible active sites: 1.95x106 – 6x109
Possible HEA/HEO: 30.201
(possible HEA/HEO) x (possible active sites) ⇒ (possible pathways)
Chen, Wei, et al. "A map of single-phase high-entropy alloys." Nature Communications 14.1 (2023): 2856.
30.201 potential single-phase equimolar alloys in body-centred cubic structures.
5% of the possible combinations

## Slide 28
Material discovery - Big-data-driven challenges
DFT and quantum modelling proposed workflow
Goal
Most probable OER pathway for a given HEO surface.
Most promising HEO compound
Plan
DFT: Binding energies (Eprod − Ereact) for particular OER steps.
Compare the energy-based probabilities of all possible reaction pathways.
Big-data driven challenges:
HEO unit(super)cells are huge
number of possible pathways is huge
computationally demanding (>5.000 years)
poorly described correlation electrons
(chemical reactions)
“Standard” DFT approach

## Slide 29
DFT and quantum modelling proposed workflow
“Standard” DFT approach
An AI/ML-aided pathway:
Reducing the number of binding-energy calculations
Material discovery - Big-data-driven challenges

## Slide 30
DFT and quantum modelling proposed workflow
“Standard” DFT approach
Quantum algorithms for the future:
Decreasing the required computational time.
Correlated effects included
(correlated electrons/chemical reactions)
The quantum algorithms need to be developed before the respective hardware is capable of tackling the real problem.
Material discovery - Big-data-driven challenges

## Slide 31
DFT and quantum modelling proposed workflow
“Standard” DFT approach
A combined
AI/ML
Quantum modelling approach
Material discovery - Big-data-driven challenges